Supplement Materials to the article

Non-model Calculation of Fusibility Diagrams  of Quasi-simple Systems From Data on Binary Subsystems

Fig S1. Solubility diagram of the NaCl – KCl – H2O system at 25°C. Stars and thick lines are calculations; black dots are aggregated experimental data [17]; thin straights are water isoactivity lines with indication of ln aw values.

Fig.S2.	Calculation from binary subsystems of the dependence of partial pressures of water (blue lines and circles), of HCl (red lines and circles), and total pressure (magenta lines and circles) along the saturated solution branch in the HCl – KCl – H2O system at 25°C. Solid circles are experimental data from [15].

Fig.S3.	Fusibility diagram for binary subsystems of ternary system Na2CO3-NaF-NaCl (open circles and lines - calculation, red circles – experimental data from [28-45]).

Ternary system Na2CO31-NaF2-NaCl(3)

Table S1.	Individual properties of components.

| Component | Heat of fusion ∆Hifus (kJ/mole) | Temperature of fusion Tifus (K) |
| --- | --- | --- |
| NaF | 33.45 | 1268 |
| NaCl | 28.04 | 1074 |
| Na2CO3 | 32.65 | 1127 |
| BaF2 | 28.47 | 1641 |
| CaF2 | 29.71 | 1691 |
| KF | 28.50 | 1119 |
| KCl | 25.50 | 1049 |
| LiF | 27.08 | 1118 |
| RbF | 19.01 | 1068 |

Table S2.	Non-ideality  parameters and eutectics coordinates for the binary subsystems.

| Binary subsystem | φ (a.u.) | Eutectic temperature Te(K) (calculation) | Eutectic composition Xieut(a.u.) (calculation) | References |
| --- | --- | --- | --- | --- |
| NaF-NaCl | 0.950 | 957 | XNaFeut= 0.34 | [28-35] |
| NaCl-Na2CO3 | 1.026 | 908 | XNaCleut= 0.56 | [28, 36-41] |
| NaF-Na2CO3 | 1.090 | 970 | XNaFeut= 0.40 | [28, 42-45] |

Table S3. Calculated Binary Diagrams (here and after Italic font corresponds to the super-cooled metastable melts).

NaF-NaCl

| T(K) | XNaF (mol.fr.) | solid phase | T(K) | XNaF (mol.fr.) | solid phase |
| --- | --- | --- | --- | --- | --- |
| 1268 | 1,00000 | NaF | 1074 | 0,00000 | NaCl |
| 1250 | 0,95302 | NaF | 1070 | 0,01229 | NaCl |
| 1230 | 0,90191 | NaF | 1050 | 0,07280 | NaCl |
| 1210 | 0,85199 | NaF | 1030 | 0,13175 | NaCl |
| 1190 | 0,8033 | NaF | 1010 | 0,18906 | NaCl |
| 1170 | 0,75586 | NaF | 990 | 0,24467 | NaCl |
| 1150 | 0,70973 | NaF | 970 | 0,29853 | NaCl |
| 1130 | 0,66492 | NaF | 957 | 0,33710 | NaF+NaCl |
| 1110 | 0,62148 | NaF | 950 | 0,35057 | NaCl |
| 1090 | 0,57944 | NaF | 930 | 0,40075 | NaCl |
| 1070 | 0,53883 | NaF | 910 | 0,44899 | NaCl |
| 1050 | 0,49969 | NaF | 890 | 0,49526 | NaCl |
| 1030 | 0,46203 | NaF | 870 | 0,53951 | NaCl |
| 1010 | 0,42588 | NaF | 850 | 0,58169 | NaCl |
| 990 | 0,39128 | NaF | 830 | 0,62175 | NaCl |
| 970 | 0,35823 | NaF | 810 | 0,65968 | NaCl |
| 957 | 0,33710 | NaF+NaCl |
| 950 | 0,32675 | NaF |
| 930 | 0,29687 | NaF |
| 910 | 0,26858 | NaF |
| 890 | 0,24190 | NaF |
| 870 | 0,21682 | NaF |
| 850 | 0,19335 | NaF |
| 830 | 0,17146 | NaF |
| 810 | 0,15116 | NaF |

NaCl-Na2CO3

| T(K) | XNaCl (mol.fr.) | solid phase | T(K) | XNaCl (mol.fr.) | solid phase |
| --- | --- | --- | --- | --- | --- |
| 1127 | 0,00000 | Na2CO3 | 1074 | 1,00000 | NaCl |
| 1110 | 0,05071 | Na2CO3 | 1070 | 0,98862 | NaCl |
| 1090 | 0,10894 | Na2CO3 | 1050 | 0,9324 | NaCl |
| 1070 | 0,16557 | Na2CO3 | 1030 | 0,87738 | NaCl |
| 1050 | 0,22056 | Na2CO3 | 1010 | 0,82363 | NaCl |
| 1030 | 0,27385 | Na2CO3 | 990 | 0,77119 | NaCl |
| 1010 | 0,32539 | Na2CO3 | 970 | 0,72014 | NaCl |
| 990 | 0,37513 | Na2CO3 | 957 | 0,68772 | NaCl |
| 970 | 0,42303 | Na2CO3 | 950 | 0,67053 | NaCl |
| 957 | 0,45316 | Na2CO3 | 930 | 0,62242 | NaCl |
| 950 | 0,46905 | Na2CO3 | 910 | 0,57588 | NaCl |
| 930 | 0,51314 | Na2CO3 | 908 | 0,56000 | NaCl+ Na2CO3 |
| 910 | 0,55526 | Na2CO3 | 890 | 0,53096 | NaCl |
| 908 | 0,56000 | Na2CO3 + NaCl | 870 | 0,48772 | NaCl |
| 890 | 0,59539 | Na2CO3 | 850 | 0,44621 | NaCl |
| 870 | 0,6335 | Na2CO3 | 830 | 0,40649 | NaCl |
| 850 | 0,66956 | Na2CO3 | 810 | 0,3686 | NaCl |
| 830 | 0,70355 | Na2CO3 |
| 810 | 0,73547 | Na2CO3 |

NaF-Na2CO3

| T(K) | XNaF (mol.fr.) | solid phase | T(K) | XNaF (mol.fr.) | solid phase |
| --- | --- | --- | --- | --- | --- |
| 1268 | 1,00000 | NaF | 1127 | 0,00000 | Na2CO3 |
| 1250 | 0,95893 | NaF | 1110 | 0,04780 | Na2CO3 |
| 1230 | 0,91395 | NaF | 1090 | 0,10288 | Na2CO3 |
| 1210 | 0,8697 | NaF | 1070 | 0,15666 | Na2CO3 |
| 1190 | 0,82622 | NaF | 1050 | 0,20907 | Na2CO3 |
| 1170 | 0,78353 | NaF | 1030 | 0,26008 | Na2CO3 |
| 1150 | 0,74168 | NaF | 1010 | 0,30962 | Na2CO3 |
| 1130 | 0,7007 | NaF | 990 | 0,35764 | Na2CO3 |
| 1110 | 0,66063 | NaF | 970 | 0,40410 | NaF+ Na2CO3 |
| 1090 | 0,62151 | NaF | 957 | 0,43343 | Na2CO3 |
| 1070 | 0,58337 | NaF | 950 | 0,44894 | Na2CO3 |
| 1050 | 0,54626 | NaF | 930 | 0,49212 | Na2CO3 |
| 1030 | 0,51020 | NaF |  |  |  |
| 1010 | 0,47523 | NaF | 910 | 0,53359 | Na2CO3 |
| 990 | 0,44139 | NaF | 890 | 0,57331 | Na2CO3 |
| 970 | 0,40872 | NaF+ Na2CO3 | 870 | 0,61125 | Na2CO3 |
| 957 | 0,38812 | NaF | 850 | 0,64736 | Na2CO3 |
| 950 | 0,37724 | NaF | 830 | 0,68161 | Na2CO3 |
| 930 | 0,34698 | NaF | 810 | 0,71399 | Na2CO3 |
| 910 | 0,31798 | NaF |
| 890 | 0,29027 | NaF |
| 870 | 0,26386 | NaF |
| 850 | 0,23878 | NaF |
| 830 | 0,21505 | NaF |
| 810 | 0,19267 | NaF |

Table S4.	Composition of melts in ternary system Na2CO3-NaF-NaCl (geometric calculation).

| T(K) | XNa2CO3 (mol.fr.) | XNaF (mol.fr.) | XNaCl (mol.fr.) | Solid phases |
| --- | --- | --- | --- | --- |
| 908 | 0,43110 | 0,00000 | 0,5611 | NaCl+Na2CO3 |
| 890 | 0,40713 | 0,06537 | 0,5275 | NaCl+Na2CO3 |
| 870 | 0,37188 | 0,14786 | 0,48026 | NaCl+Na2CO3 |
| 853 | 0,34311 | 0,22258 | 0.43421 | NaCl+NaF+Na2CO3 |
| 957 | 0,00000 | 0,34005 | 0,65995 | NaCl+NaF |
| 950 | 0,00937 | 0,32751 | 0,66312 | NaCl+NaF |
| 930 | 0,05342 | 0,30097 | 0,64561 | NaCl+NaF |
| 910 | 0,12992 | 0,27799 | 0,59209 | NaCl+NaF |
| 890 | 0,20196 | 0,25566 | 0,54238 | NaCl+NaF |
| 870 | 0,27015 | 0,23408 | 0,49576 | NaCl+NaF |
| 853 | 0,34311 | 0,22258 | 0.43421 | NaCl+NaF+Na2CO3 |
| 971 | 0,59931 | 0,40069 | 0,00000 | NaF+Na2CO3 |
| 970 | 0,57766 | 0,40756 | 0,01478 | NaF+Na2CO3 |
| 950 | 0,53519 | 0,37014 | 0,09467 | NaF+Na2CO3 |
| 930 | 0,49417 | 0,33479 | 0,17104 | NaF+Na2CO3 |
| 910 | 0,45464 | 0,30151 | 0,24385 | NaF+Na2CO3 |
| 890 | 0,41667 | 0,2703 | 0,31304 | NaF+Na2CO3 |
| 870 | 0,38028 | 0,24112 | 0,37860 | NaF+Na2CO3 |
| 853 | 0,34311 | 0,22258 | 0.43421 | NaCl+NaF+Na2CO3 |

Table S5.	Composition of melts in ternary system Na2CO3-NaF-NaCl (thermodynamic calculation).

| T(K) | XNa2CO3 (mol.fr.) | XNaF (mol.fr.) | XNaCl (mol.fr.) | Solid phases |
| --- | --- | --- | --- | --- |
| 908 | 0,44000 | 0,00000 | 0,56000 | NaCl+Na2CO3 |
| 890 | 0,40313 | 0,07742 | 0,51945 | NaCl+Na2CO3 |
| 870 | 0,36423 | 0,15968 | 0,47610 | NaCl+Na2CO3 |
| 853 | 0,34 | 0,23 | 0.43 | NaCl+NaF+Na2CO3 |
| 957 | 0,00000 | 0,33700 | 0,66300 | NaCl+NaF |
| 950 | 0,02729 | 0,32672 | 0,64600 | NaCl+NaF |
| 930 | 0,10325 | 0,29826 | 0,59849 | NaCl+NaF |
| 910 | 0,17618 | 0,27120 | 0,55262 | NaCl+NaF |
| 890 | 0,24603 | 0,24554 | 0,50844 | NaCl+NaF |
| 870 | 0,31271 | 0,22129 | 0,46600 | NaCl+NaF |
| 853 | 0,33908 | 0,23149 | 0,42943 | NaCl+NaF+Na2CO3 |
| 970 | 0,59100 | 0,40900 | 0,00000 | NaF+Na2CO3 |
| 950 | 0,54269 | 0,37478 | 0,08252 | NaF+Na2CO3 |
| 930 | 0,49651 | 0,34214 | 0,16135 | NaF+Na2CO3 |
| 910 | 0,45248 | 0,3111 | 0,23642 | NaF+Na2CO3 |
| 890 | 0,41064 | 0,28166 | 0,30770 | NaF+Na2CO3 |
| 870 | 0,37101 | 0,25385 | 0,37514 | NaF+Na2CO3 |
| 853 | 0,33908 | 0,23149 | 0,42943 | NaCl+NaF+Na2CO3 |

Table S6.	Composition of melts in ternary system  CaF2-NaF-BaF2 (thermodynamic calculation).

| T(K) | XCaF2 (mol.fr.) | XNaF (mol.fr.) | XBaF2 (mol.fr.) | Solid phases |
| --- | --- | --- | --- | --- |
| 1079 | 0,36500 | 0,63501 | 0,00000 | CaF2+NaF |
| 1070 | 0,35855 | 0,62160 | 0,01985 | CaXBa1-XF2+NaF |
| 1055 | 0,33988 | 0,58452 | 0,07560 | CaXBa1-XF2+NaF |
| 1040 | 0,32476 | 0,55389 | 0,12134 | CaXBa1-XF2+NaF |
| 1025 | 0,30638 | 0,51804 | 0,17558 | CaXBa1-XF2+NaF |
| 1003 | 0.26 | 0.44 | 0.30 | CaXBa1-XF2+BaXCa1-XF2+NaF |
| 1091 | 0,00000 | 0,61300 | 0,38700 | BaF2+NaF |
| 1070 | 0,04689 | 0,58182 | 0,37129 | BaXCa1-XF2+NaF |
| 1055 | 0,09990 | 0,54717 | 0,35293 | BaXCa1-XF2+NaF |
| 1040 | 0,15208 | 0,51321 | 0,33471 | BaXCa1-XF2+NaF |
| 1025 | 0,20333 | 0,47999 | 0,31668 | BaXCa1-XF2+NaF |
| 1010 | 0,24556 | 0,45238 | 0,30206 | BaXCa1-XF2+NaF |
| 1003 | 0.26 | 0.44 | 0.30 | CaXBa1-XF2+BaXCa1-XF2+NaF |
| 1277 | 0,49592 | 0,00000 | 0,50508 | CaXBa1-XF2 +BaXCa1-XF2 |
| 1200 | 0,45292 | 0,08315 | 0,46393 | CaXBa1-XF2 +BaXCa1-XF2 |
| 1150 | 0,40203 | 0,18411 | 0,41386 | CaXBa1-XF2 +BaXCa1-XF2 |
| 1100 | 0,35319 | 0,28126 | 0,36555 | CaXBa1-XF2 +BaXCa1-XF2 |
| 1050 | 0,30664 | 0,37410 | 0,31925 | CaXBa1-XF2 +BaXCa1-XF2 |
| 1003 | 0.26 | 0.44 | 0.30 | CaXBa1-XF2+BaXCa1-XF2+NaF |

Table S7.	Literature and average - optimal (highlight) Heats of Fusion for Hydrocarbons.

| Component | Heat of fusion ∆Hf (kJmole) | Literature | Component | Heat of fusion ∆Hf (kJmole) | Literature |
| --- | --- | --- | --- | --- | --- |
| n-C5H12 | 8.38 -8.41 8.4 | [81, 82] | n-C6H14 | 13.06 – 13.10 13.1 | [83, 84] |
| n-C7H16 | 14.03 - 14.14 14.1 | [85, 86] | n-C8H18 | 20.09 – 21.80 21.8 | [87-89] |
| n-C9H20 | 15.45 – 22.12 22.1 | [90-92]* | n-C10H22 | 28.72 28.7 | [93] |

*Used data [92], which takes into account heat of polymorph transformation.